## Slide 1: Intermodal TFM with Applications to Weld Inspections
Renato Nogueira – Sonatest AP
renato.nogueira@sonatest.com

## Slide 2
SIMPLICITY
  Customer support by people who care.
  Solutions with clever design for smooth operations.
CAPABILITY
  Global network with partners in more than 50 countries.
  Product development based on technology innovations.
RELIABILITY
  Business relationship based on trust and confidence.
  Products built to withstand the NDT real life conditions.
A brand that stands strong over years for the quality of its people & values
MOTTO

## Slide 3
Introduction to TFMi
    Objective: Improve the TFM Readout
    TFMi Image Processing
    Proof of concept
Intermode on Real Flaws – Geometric Fidelity
    7 Defect Images
Quantitative Results
    Sensitivity
    Signal to Noise Levels
    Height Sizing
    Sharpness Advantage
New Considerations
    SDH Reflector
    Calibration
    Velocity, Probe Zero & Thickness
Conclusion
Agenda

## Slide 4
1. Introduction to TFMiTM

## Slide 5
1.1 TFMiTM : TFM Intermode
TFMi imaging is a new way to combine live TFM modes.
TFM is the most recent and natural transition from sectorial and linear scans.
Known advantages of TFM:
  Apply focus delays to all the pixels.
  The image represents one ultrasound propagation mode

## Slide 6
1.1 TFMiTM Objectives
Why not use more modes?
  Hypothesis: a reflector may generate many echo signals from different propagation modes. By combining these modes, it should enhance the image quality and be closer to is real shape and orientation.
  2 methods are available: Keep Max and Product.
Our recent study introduces the Intermode product technique.
  We targeted flat weld inspections

## Slide 7
1.2 TFM Image Processing
FMC Acquisition
ROI Imaging
Display
= Rx A-Scan
= Tx Element

## Slide 8
1.2 TFMiTM Image Processing (Product Operator)
FMC Acquisition
Many ROI’s Imaging
Combining Pixels
Display

## Slide 9
1.2 TFMiTM Image Parameters
Enable the TFMi mode.
Add up to 4 propagation modes that is realistically useful
Set the Intermode operator (keep max or product)

## Slide 10
1.3 Proof of concept

## Slide 11
1.3 TFMi Live Data Streaming
=
High Fidelity Center Line Crack Image

## Slide 12
2. Intermode on Real Weld Flaws
Setup: 7.5 MHz, 0.6 mm pitch, 44E aperture, 60S Wedge

## Slide 13
2. Intermode on Real Weld Flaws

## Slide 14
2. Intermode on Real Weld Flaws

## Slide 15
2. Intermode on Real Weld Flaws
Effortless Characterisation based on a “simple” image
  Less result interpretation and guess during the inspections
  Better customers’ confidence in regards of the ultrasound data.
Maximise your current probes, 32E probe performance is getting closer to the 64E models!
TFM has never been so close to reality. You can see what the defect profiles look like.

## Slide 16
3.1 Sensitivity
Keep Max = No sensitivity loss
  It is like a folded TFM
  For e.g., when you do TT/TTTT/6T, it is a 3-skip TT folded TFM.
Product; Require about +15 dB of scanning gain.
  TFM image is never noise free and always positive
  All near zeros modes will not amplify the background noise but will reduce it.
TFMi Images are closer to a binary-colored image. Like a photo, there is an object, or not!

## Slide 17
3.2 Signal to Noise Levels
Low amplitude pixels decrease noise levels
The product effect is very close to the geometric mean filtering

## Slide 18
3.3 Height Sizing
In this experience, we also compared to a 15 MHz TOFD scan.
Among all TFM and Intermode techniques, the closer height evaluation to TOFD was TFMi.
TFMi deviation was 17% better than TFM.
  Standard deviation of all TFM modes to all defects 1.0 mm (0.004 inch)
  Standard deviation of all TFMi scans is 0.83 mm (0.0033 inches)
TFMi does not have the TOFD intrinsic lateral wave limitations.
  Lateral wave hides surface and useful signals.

## Slide 19
3.4 Sharpness Advantage

## Slide 20
3.4 Sharpness Advantage
TFMi echo width = 0.28 mm
PA TTTT echo width = 0.45 mm
Sharper Contour (Slope)
  Better Height Sizing

## Slide 21
4 New Considerations
SDH Reflector
Calibration
Velocity, Probe Zero and Thickness

## Slide 22
4.1 Side Drilled Hole in TFMi
Image comparison and -6 dB height evaluation; TT, TTTT, TT/TTTT and TT/TTT/TTTT over a 2 mm SDH
Same Setup:
7.5 MHz, 0.6 mm pitch, 44E aperture, 60S Wedge. 8 mm Index Offset

## Slide 23
4.2 Calibrations
TFMi scan cannot be a amplitude based technique. The scanning gain parameter is more a brightness correction.
Amplitude fidelity check still works.
Radius reflector strictly works with the TT mode. Adding more modes on radius provides no advantages.

## Slide 24
4.3 Velocity, Probe Zero and Thickness
TFMi creates sharp images. This requires also a precise Velocity and Probe zero calibration.
An incorrect thickness parameter will result in a faulty scan plan.
  This is particularly problematic for those propagation modes assuming a backwall reflection on the pulse or returning wavefront.
5T Wall Reflections

## Slide 25
Conclusion
The evolution of ultrasound techniques is thrilling and faster than ever!

## Slide 26
Conclusion
TFMi is superior on weld analysis.
  SNR for a cleaner image
  Better flaw shape accuracy
Defect characterisation and precise height dimension facilitate critical assessment.
TFMi offers to the user to check and merge many modes at the same time.
  TFMi may not work by using less favorable modes.

## Slide 27
Contact us to find your ultrasonic NDT solutions!
Sonatest (Headquarters)
  Milton Keynes, United Kingdom
  t: +44 (0) 1908 316345
  e: sales@sonatest.com
Sonatest USA
  San Antonio Texas, United States
  t: +1 (210) 697 0335
  e: sales@sonatestinc.com