## Slide 1: Inspection Techniques and Application Solutions Supported by New Generation PA UT Technology
Guy Maes
Eddyfi Technologies
Notes: Duration 15”
Good morning Ladies and Gentlemen,
This presentation will be about “Inspection Techniques and Application Solutions supported by New Generation PA UT Technologyʺ

## Slide 2
Introduction : recent technology progress
FMC, PWI, and advanced imaging techniques
Hardware innovation
Case studies : thick plate weld, DM weld
Conclusions
Overview
Notes: Duration 45”
So let’s start with the overview of my presentation
First of all I present a short introduction on recent progress in phased array UT technology.
I will then review the basic principles of FMC and PWI firing modes, and some advanced imaging techniques like TFM
After that, I will briefly talk about our newest phased arrray unit, that allows to deploy this new technology.
The largest part of my presentation will be about the results of case studies that we conducted to validate the benefits of the new tools involving FMC, PWI and advanced imaging techniques.
Finally, I will present some conclusions from our work.

## Slide 3
PA UT is a mature and widely adopted technology allowing for efficient inspections of critical components in various industries
Over the last 5 years, FMC and live TFM have been available on high-end PA UT units, and have been introduced in ASME code and ISO standards
Dedicated training courses are offered by large training centers
Innovation is still on-going :
  Ease of use
  Inspection speed
  Image quality
Introduction – Recent Technology Progress
Notes: Duration 50”
It is fair to say that PA UT is a mature and widely adopted technology allowing for efficient inspections of critical components in various industries.
Over the last 5 years, new techniques, FMC and live TFM have been available on high-end PA UT units. They have been introduced in the ASME Code Section V Article 4, Mandatory Appendix XI, and in the ISO standard (documents 23864 and 23865)
Dedicated training courses as prescribed by the codes, are being offered by the large training schools
But innovation is still on-going, and NDE equipment vendors are contantly working on making the inspections easier to setup, increase the inspection speed, and improve the imaging quality
In my presentation today I will show the results of our efforts over the last 2 years.

## Slide 4
FMC consists in capturing and recording A-Scan signals from every transmitter-receiver pair in the array
From the raw A-scan signals, it is possible to generate UT imaging with advanced focusing techniques (like TFM), live or through post processing
FMC – Basic Principles
Notes: Duration 40”
Let us briefly review some basic principles
Full Matrix Capture (FMC) is a firing technique that consists in capturing and recording A-Scan signals from every transmitter-receiver pair in an array.
Each element of the probe is fired sequentially. For each element pulsed, every receiving element collects an individual A-scan.
At the end of the sequence for a probe with 64 elements we have recorded a matrix of 4096 A-scan signals.
From the raw A-scan signals, it is then possible to generate UT imaging with advanced focusing techniques (like TFM), live or through post processing.

## Slide 5
Multi-element aperture firing technique (often full aperture), while receiving with each element individually
Multiple focal laws can be fired with varying angle or aperture
Like for FMC, live TFM imaging can be done during inspection
PWI (Plane Wave Imaging) – Basic Principles
Notes: Duration 30”
Plane Wave Imaging (PWI) is an alternative firing technique that uses a multi-element aperture for pulsing instead of firing each element individually like FMC. Receiving is done with each element individually.
The firing sequence typically consists of multiple focal laws, with varying angle and/or aperture.
Like for FMC, live TFM UT imaging can be done during inspection.

## Slide 6
High energy excitation provides greater sensitivity and better SNR
Higher PRF and scanning speed because of significantly shorter firing sequence and less elementary signals to process
Significantly smaller data file size for raw data saving
PWI (Plane Wave Imaging) – Benefits
Notes: Duration 35”
PWI data acquisition has several benefits compared to FMC data recording:
The emitted pulse from the full aperture has more energy and is more directional than a single element excitation. It provides greater sensitivity and better SNR together with higher PRF and scanning speed because of significantly shorter firing sequence and less elementary signals to process.
At the same time, less elementary A-scans recorded mean a significantly smaller data file for raw data saving.

## Slide 7
Total Focusing Method (TFM)
Live FMC or PWI data reconstruction, dedicated focal laws for each pixel
Images (TFM frames) built with ideally focused PA UT signals in each pixel
Excellent resolution for better characterization and sizing of challenging flaws
Advanced Focusing Techniques - TFM
Notes: Duration 45”
The most commonly used advanced focusing algorithm is the Total Focusing Method or TFM
This algorithm sums the elementary A-scans signals from all elements in the array to generate a frame of pixels, where each pixel is computed using a dedicated focused focal law. The TFM frames can be used for “live” interpretation, or they can be stored for each position of the probe, very similar to a “dynamic” merge view in regular phased array.
The process results in nearly ideal focusing in each point of the image, and this improved image resolution can allow for better characterization and sizing of challenging flaws.

## Slide 8
TFM Envelope image is obtained from the magnitude of the summed analytic signals (from Hilbert transform)
Image looks like PA UT with smoothing filter applied
Allows to obtain the same Amplitude Fidelity, while using larger pixel size
Benefits:
  Increased scanning speed (reduced frame size)
  Enhanced image quality
Live TFM Envelope – Principles & Benefits
Notes: Duration 45”
The Envelope is a recently introduced feature for live TFM .
The TFM Envelope is obtained from the magnitude of the summed analytic signals through a Hilbert transform. The resulting live TFM images look like phased array signals with a smoothing filter applied.
The Envelope delivers the same Amplitude Fidelity as the regular TFM reconstruction, while using larger pixel size. Larger pixel size means that we can use a lower resolution, and increase the scanning speed with any loss in inspection quality. Typically, the use of the Envelope will allow a reduction of the frame size by a factor 4.
Another benefit is the improvement of the image quality.

## Slide 9
Eddyfi’s newest compact PA UT system, offering very high performance for the most challenging inspections
High-speed data transfer : up to 150 MB/s for FMC raw data, PA UT data, live TFM and live PWI
PA UT 64/128PR + 2 UT (TOFD)
Rugged casing
No air intake, IP65 rating design
Powered by UltraVision Classic
Notes: Duration 50”
The EMERALD is Eddyfi’s newest compact phased array UT system, and it includes all the advanced tools that I have just discussed.
It allows for high-speed data transfer (up to 150 Mbytes/s), through a 5 Gigabit Ethernet (5 Gbit/s) connection for FMC elementary A-scans, phased array UT data and live TFM data.
The EMERALD is a phased array 64/128PR with 2 separate conventional UT channels extremely well-suited to perform TOFD
It comes in a rugged casing, there is no air intake, and the unit is designed for IP65 rating.
EMERALD is powered by UltraVision Classic, so it offers to the user all the benefits from this complete phased array UT and FMC/TFM inspection package.

## Slide 10
Case Study - Live TFM Envelope
ASTM E2491 reference block, pulse-echo, L-waves
TFM L-L 256 x 256
Max. Acq. Rate = 53 Hz
AF = 1.8 dB
Notes: Duration 45”
In the first case study I will illustrate how the TFM Envelop allows to speed up the inspection of a 60 mm thick carbon steel component, while maintaining the image quality.
For this purpose, I will use the live TFM images of a set of small side-drilled holes in the ASTM E2491 reference block.
When we use a 256 by 256 frame in L-L mode, the Amplitude Fidelity criterium of 2 dB is just satisfied, and it allows for a maximum acquisition rate just above 50 Hz. Still, when we zoom in on the reflectors, the image quality is not really optimal.

## Slide 11
Case Study - Live TFM Envelope
ASTM E2491 reference block, pulse-echo, L-waves
TFM L-L 512 x 512
Max. Acq. Rate = 26 Hz
AF = 0.4 dB
Notes: Duration 15”
When switching to a 512 by 512 frame, the Amplitude Fidelity improves to 0.4 dB, and also the image quality clearly improves.
Unfortunately, the maximum acquisition rate is reduced by a factor 2, to 26 Hz.

## Slide 12
Case Study - Live TFM Envelope
ASTM E2491 reference block, pulse-echo, L-waves
TFM L-L 256 x 256
Max. Acq. Rate = 53 Hz
AF = 0.4 dB
Notes: Duration 25”
We can see that using the Envelope feature on a 256 by 256 frame will also provide an Amplitude Fidelity criterium of 0.4 dB, and a high quality image. In addition, the maximum acquisition rate of 53 Hz is maintained.

## Slide 13
Case Study – PWI vs. FMC Firing Sequence
ASTM E2491 reference block, pulse-echo, L-waves
Full aperture firing sequence
Azimuthal 7 Laws
Notes: Duration 20”
Let us stay with the same probe configuration and specimen, and compare the use of a PWI firing sequence versus a complete FMC firing sequence
The PWI firing sequence is an azimuthal sweep of 7 angles, using the full aperture of the probe.

## Slide 14
Case Study – PWI vs. FMC Firing Sequence
ASTM E2491 reference block, pulse-echo, L-waves
Max. Acq. Rate = 53 Hz
AF = 0.4 dB
Max. Acq. Rate = 179 Hz
AF = 0.4 dB
Notes: Duration 30”
On this slide we can see the images from 256 x 256 TFM L-L frames, on another set of side-drilled holes in the ASTM reference specimen.
The image on the left side is the PWI/TFM with Envelope while the FMC/TFM with Envelope is shown on the right.
The Amplitude Fidelity is the same, and we can see that image quality is comparable.

## Slide 15
Case Study – PWI vs. FMC Firing Sequence
ASTM E2491 reference block, pulse-echo, L-waves
Max. Acq. Rate = 53 Hz
AF = 0.4 dB
Max. Acq. Rate = 179 Hz
AF = 0.4 dB
1.1 mm
Notes: Duration 20”
And when zooming in on the two 1 mm diameter side-drilled holes that are only slightly more than a mm a part, we can see that they are clearly resolved in both cases.
But the maximum acquisition rate for the PWI firing sequence is more than 3 times higher, which will allow for a 3 times faster inspection.

## Slide 16
Case Study – Live FMC/TFM Multi-Probe and TOFD
Two-sided live TFM weld inspection (2 x 256 kpixel frames) & TOFD
Upstream
TFM T-T
Downstream
TFM T-T
TOFD
Upstream
TFM T-T
Downstream
TFM T-T
TOFD
Notes: Duration 1’00”
Let’s now move on to a more realistic case, the inspection of a carbon steel plate weld with a V-bevel, containing and 4 typical realistic welding defects
Using its high-speed data transfer and onboard processing, the EMERALD is capable of running multi-probe live TFM.
This example shows a setup and results from a two-sided TFM weld inspection combined with TOFD. We are looking at full skip images from the TFM T-T wave mode, and the TOFD signal in the middle. The 4 welding flaws are easily detected.
When using the TFM Envelope, this two-sided inspection can be run at more than 20 mm/s, while satisfying the Amplitude Fidelity criterion of the ASME Code

## Slide 17
Case Study – Live PWI/TFM Multi-Mode
T-T mode
TT-TT mode
TT-T mode
Live PWI/TFM weld inspection, multi-mode T-T, TT-TT, TT-T
Notes: Duration 1’00”
Let’s continue to work with this carbon steel plate weld.
With both FMC and PWI firing sequences, we can also generate live TFM data according to multiple reconstruction modes. This is a very powerful inspection tool, because the detection capability of the different reconstruction modes is often complementary.
In this example I am showing multi-mode PWI/TFM with 3 TFM frames of 65 kpixels (256 x 256 pixels). The 3 wave modes have been recorded simultaneously, showing the specific detection capability of each wave mode.
A two-sided inspection with 3 PWI/TFM modes from each side can be run at more than 45 mm/s, which is 3 times faster than with FMC/TFM in similar conditions.

## Slide 18
“Regular” TFM - DAS (Delay And Sum) - sums delayed pulser-receiver A-Scans
TFM DMAS (Delay Multiply And Sum) - sums delayed pulser-receiver A-Scans multiplied by each other (correlation), to reduce TFM artifacts due to “partially constructive” interferences
TFM with PCF (Phase Coherence Factor) - reduces sidelobes of the image by including phase coherence information
TFM Envelope – can be applied with either DAS, DMAS and PCF
Notes: Duration 1’30”
The case studies that we have discussed up to now involved live TFM processing of the FMC or PWI raw data
But in some cases, specifically for challenging flaws and damage mechanisms, it can be useful to record the raw FMC data for offline processing. The UltraVision Classic software allows to reconstruct various types of data groups from the raw FMC data, including standard phased array signals, TFM (Total Focusing Method) frames or STF (Sectorial Total Focusing) images.
A number of TFM reconstruction algorithms are available:
DAS (Delay And Sum)
This is the most commonly used TFM reconstruction algorithm. It basically applies appropriate delays to the individual pulser-receiver A-scan, and sums them afterwards.
DMAS (Delay Multiply And Sum)
This algorithm sums the delayed pulser-receiver A-Scans multiplied by each other. This process reduces the well-known TFM artifacts that are in fact “partially constructive” interferences, often occurring in the presence of large reflectors like the back-wall of a component.
TFM with PCF (Phase Coherence Factor)
TFM with Phase Coherence Factor reduces the sidelobes of the imaging by including phase coherence information
TFM Envelope is also available offline, and can be applied with either DAS, DMAS or PCF.

## Slide 19
Case Study – FMC Data Reconstruction
Target Reflectors
Small low-reflectivity targets (*) near calibration SDH and back-wall
Aluminum specimen, T = 48 mm, LM 5 MHz in contact
(*) regular conical holes, drilled from ID
Notes: Duration 30”
As an example, we will look at the TFM imaging of small, low-reflectivity targets close to large geometrical reflectors.
We took an aluminum calibration block with two side-drilled holes, and added multiple small holes, drilled from the ID. The end of these regular drilled holes is conical, and therefore they are very poor reflectors.
A standard LM 5 MHz probe was used in contact with the specimen.

## Slide 20
Case Study – FMC Data Reconstruction
TFM 1 Mpixel
DMAS & Envelope
TFM 1 Mpixel
DMAS
Live TFM 65k (256 x 256)
TFM 1 Mpixel Regular (DAS)
TFM 1 Mpixel
Envelope
TFM 1 Mpixel
PCF & Envelope
Reference Gain
Notes: Duration 20”
This slide shows images of the region of interest in the L-L wave mode, from live TFM and 5 reconstruction algorithms that we saw in the previous example. The gain setting was adjusted to bring the calibration SDH to roughly 80% FSH.

## Slide 21
Case Study – FMC Data Reconstruction
TFM 1 Mpixel
DMAS & Envelope
TFM 1 Mpixel
DMAS
Live TFM 65k (256 x 256)
TFM 1 Mpixel Regular (DAS)
TFM 1 Mpixel
Envelope
TFM 1 Mpixel
PCF & Envelope
Reference Gain + 12 dB
Notes: Duration 1’15”
Typically, when looking at challenging damage mechanisms with low reflectivity, operators need to apply increased gain settings.
On the images with increased softgain, the typical TFM artifacts generated by strong geometrical reflectors like the back-wall and large SDH’s become visible on the live TFM image, and the regular reconstructed TFM image.
The envelope adds smoothing to the image but doesn’t reduce the artifacts.
In real live inspections the artifacts will jeopardize reliable detection of small low-reflectivity reflectors.
On the three images below, we can see that DMAS and the Phase Coherence Factor strongly reduce the artifacts, and thus improve the SNR of the global image. The envelope can also be applied together with those 2 algorithms to obtain the smoothened images.
When zooming in we can better see the small low-reflectivity indications adjacent to the strong geometrical reflectors.

## Slide 22
Case Study – FMC Data Reconstruction
DM weld specimen, T = 1.2 in
1.5 MHz dual matrix array (DMA) probe, 2 x (10 x 6) elements, TRL mode
(Courtesy of EPRI and Nucleom)
Dissimilar metal weld, branched ID crack, DMA 1.5 MHz
Notes: Duration 40”
My last case study is the inspection of a complex dissimilar metal weld that contains a large branched ID surface breaking crack.
The objective of the trial was to explore the potential of advanced focusing techniques for flaw characterization and sizing, using a large aperture DMA probe at 1.5 MHz. Both transmitter and receiver arrays have a 10 x 6 element configuration. This slide shows the actual probe assembly and the acoustic beam for standard PA UT focused near the ID surface.

## Slide 23
Case Study – FMC Data Reconstruction
(Courtesy of EPRI and Nucleom)
Standard PA UT
focused near ID
TFM L-L
Regular
intended crack morphology
corner
tip
corner
tip
Dissimilar metal weld, branched ID crack, DMA 1.5 MHz
Notes: Duration 40”
So let us have a look at the images obtained with the different inspection techniques.
The merged view of the standard PA UT technique is shown at the top of the slide. The corner trap is very well detected, because the lower angles of the sector scan are typicaly focused near the ID. The upper part of the crack is visible but the image is incomplete for this very high crack
The image at the bottom of the slide is the regular TFM and was processed from recorded FMC data. The image of the corner trap is almost identical, but we get a complete image of the upper part of the crack, and even some of the other facets of the crack.

## Slide 24
Case Study – FMC Data Reconstruction
(Courtesy of EPRI and Nucleom)
TFM L-L DMAS & Envelope
TFM L-L
Envelope
intended crack morphology
corner
tip
corner
tip
Dissimilar metal weld, branched ID crack, DMA 1.5 MHz
Notes: Duration 30”
And now we are looking at the TFM with Envelope at the bottom of the slide, and the TFM DMAS with Envelope at the top of the slide.
The Envelope does not have a large influence on the image quality in this case, but the DMAS algorithm provides a substantial improvement of the SNR of the image, while conserving the various facets of the crack.

## Slide 25
Advanced focusing techniques have become an important asset in the phased array UT toolkit, to improve resolution of flaw images, and inspection coverage
Active aperture and frame resolution are key parameters, and must be carefully selected to exploit full potential of advanced focusing techniques
PWI firing sequence and TFM Envelope allow to drastically increase the inspection speed
Careful probe selection (wave mode, frequency) remains a requirement for succes
When FMC raw data are available, the use of different wave modes and advanced processing algorithms can improve detection capability on challenging reflectors
Conclusions
Notes: Duration 1’00”
Based on the results of the case studies that I presented, we can draw the following conclusions:
Advanced focusing techniques have become important assets in the phased array UT toolkit; they can improve the resolution of flaw images and increase the inspection coverage with focused beams.
Active aperture and frame resolution are key parameters for the TFM technique, and must be carefully selected to exploit the full potential of the technique
The PWI firing sequence and the TFM envelope allow to drastically increase the inspection speed, while maintaining image quality
Selection of appropriate probes, in terms of frequency and wave mode, remains a mandatory requirement for succes
When FMC raw data have been collected, the use of different wave modes and advanced processing algorithms can improve detection capability on challenging reflectors

## Slide 26
Any Questions ???